## Slide 1: Materials in superconducting quantum bits by William D. Oliver and Paul B. Welander (超導量子位元中的材料)
報告者 : 謝凱閔
指導教授: 邱奎霖 教授

## Slide 2: Outline
Introduction
  What is a qubit ?
  Coherence/decoherence time
  Spectacular improvements
Josephson tunnel junctions and two-level systems
  Josephson tunnel junctions
  Two-level systems
What resonators can tell us about materials and fabrication
  Introduction of resonator
SQUIDs and flux(Skip)
  Source of noise
Summary

## Slide 3
“Superconducting artificial atoms” are electronic circuits.
What is a qubit ?
linear LC resonant circuits + Josephson junction(JJ)

## Slide 4
What is a qubit ?
“Superconducting qubit” generally refers to the ground and first-excited state of a superconducting artificial atom.
Two-Level System (TLS)
 |  | Large

## Slide 5
The amount of time that qubits stay in the superposition state is referred to as their "coherence time ".
Coherence/decoherence time
Two characteristic decay rates that contribute to coherence loss:
Γ 1 = longitudinal relaxation rate(energy decay rate)
Γ 2 = transverse relaxation rate (decoherence rate)
T =pure dephasing time

## Slide 6
Spectacular improvements
1999, Nakamura et al. : nanosecond-scale coherence in Cooper pair box(charge qubit)
2002, Vion et al. : hundreds of nanoseconds T2 in a modified charge qubit
Burkard et al. : elucidated the importance of symmetry in qubit designs
Bertet et al. : persistent-current flux qubit coherence times into the few microseconds range
In 2005–2006, Ithier et al. and Yoshihara et al. : measured the noise properties of quantronium and flux qubits
Schoelkopf et al. : developed “transmon” qubit
MIT/NEC group : 2D geometry persistent-current flux qubit(20us T2)
Yale group: developed 3D-cavity (100 20us T2)

## Slide 7
Spectacular improvements

## Slide 8
Spectacular improvements

## Slide 9
(1) Reduce the qubit’s sensitivity to a given type of noise
Design modifications
(2) Identify and reduce the sources of noise
Materials and Fabrication improvements
Spectacular improvements

## Slide 10
Josephson tunnel junctions
: junction critical current
Then
The parallel-plate-like structure
Anharmonic oscillator
Ej : Josephson coupling energy of the junction by
Ec : Electrostatic Coulomb energy

## Slide 11
Two-level systems
TLS defects is a localized low-energy excitation that is predominantly found in amorphous materials
These systems occur (1) defects in the crystal structure
(2) the presence of polar impurities such as
As the devices cools , TLS are seen as major source of noise and decoherence
TLS has a dipole moment that will interact with electromagnetic fields

## Slide 12
Two-level systems
Two primary ways that TLS in the tunnel barrier can interact with the qubit:
(1) TLS and qubit become coupled
(2) Low-frequency charge fluctuations in
the TLS critical current noise
The spectral splittings occur when the energy-level difference of the qubit matches that of a TLS in the junction barrier
Notes: (1)TLS與qubit能級間距相等形成耦合,qubit會與tls互相交換能量,而tls又會藉由聲子把能量消耗出去,造成非同調
(2)低頻率電荷擾動造成tunnel barrier的高度發生變化,使jj的𝐼_𝑐有擾動,會造成qubit能級擾動,也會非同調
調整電流偏壓,可以調整qubit的工作頻率fuw,上圖是非晶下圖是單晶
單晶的缺陷5倍小

## Slide 13
Two-level systems
Reduce TLSs’ impact:
(1) Improving the quality of barrier
(2) Smaller the junctions(0.1~0.3um)
(3) Replace the materials
(4) Change method to grow amorphous
oxide barriers
            TLSs in the junction barrier should not be ignored

## Slide 14
Introduction of resonator
Resonators identify noise sources and decoherence mechanisms. eg. TLSs
TLSs : (1) Appear in barrier of JJ and dielectric materials used in circuit
(2) Absorb and dissipate energy at low powers and low temperatures,
but will saturate as both voltage and temperature increase
As an increasing loss tangent, tan δ , with decreasing power that plateaus only at very low powers

## Slide 15
Introduction of resonator
At low powers and temperatures TLSs tend to be in their ground states can absorb energy from the resonator and dissipate that energy via phonon emission, thereby increasing the resonator loss.

## Slide 16
Introduction of resonator
Resonators are also sensitive to the TLSs that form on metal surfaces and at interfaces between the metal and substrate.
Internal factor : Q
loss (1/ Q )
Factors affecting Q quality : (1) Oxide layer on metal surface
(2) Metal-substrate
(3) Substrate-air interfaces
Dominate

## Slide 17
Introduction of resonator
Address the issue of native oxides on metal surfaces
e.g. Fabricate CPW resonators from superconducting nitrides
Address the issue of substrate/superconductor interface
e.g. Films grown on sapphire or on thick SiN layers

## Slide 18
Summary
Increasing coherence times by innovations in qubit, device fabrication, and new materials.
Eliminated many TLS sources leading to substantial increases in resonator quality factors and qubit coherence times.
Understanding the effects of decoherence mechanisms such as quasiparticle tunneling or critical current fluctuations are being revisited in more detail.